Synthesis and Characterization of Semiconducting Sinnerite (Cu6As4S9) Thin Films

Scott A. McClary and Rakesh Agrawala)

Davidson School of Chemical Engineering, Purdue University, 480 Stadium Mall Dr.,West Lafayette, IN 47907, USA.

a) Address all correspondence to this author. Email: agrawalr@purdue.edu

ABSTRACT

Sinnerite (Cu6As4S9) is a semiconductor computed to have attractive optoelectronic properties, but little attention has been paid to its experimental synthesis and characterization. Here, we report the first synthesis of polycrystalline sinnerite thin films. By heating Cu3AsS4 nanoparticles in sealed ampoules with As2S2 powder, a phase transformation to Cu6As4S9 is achieved along with the formation of micron-sized dense grains appropriate for device applications. The films display a band gap of ~1.2 eV, significant photocurrent generation under simulated AM1.5 illumination, and carrier lifetimes nearing 1 ns, demonstrating the promise of sinnerite for use in photovoltaic applications.

INTRODUCTION

Thin-film photovoltaic (PV) devices are a promising low-cost method for harvesting solar radiation and converting it into electricity that can meet the human race’s energy demands for the foreseeable future. Building on decades of laboratory-scale research, CdTe and Cu(In,Ga)Se2 solar cells have been commercialized, but their widespread deployment may be challenging due to the price volatility and relative scarcity of indium and tellurium sources.1 Thus, a significant fraction of the PV community has begun to focus on alternative materials consisting of earth-abundant elements, with substantial research into compounds that are either derivatives of existing compounds (such as Cu2ZnSn(S,Se)4)2–4 or entirely new classes of materials (such as lead halide perovskites).5 However, none have yet achieved the combination of efficiency and stability that warrant large-scale manufacturing and commercialization.

Cu-As-S compounds have recently emerged as potential PV materials due to their outstanding optoelectronic properties and constituent earth abundant elements that possess dissimilar cation sizes, a characteristic which typically results in high formation energies and hence lower concentrations of harmful antisite defects. One such compound is tetragonal luzonite (LUZ, Cu3AsS4), which has a bandgap appropriate for solar PV applications (1.15 – 1.25 eV); additionally, LUZ nanoparticle (NP) films generate more photocurrent than their antimony-based analogs.6–8 A polymorph of LUZ is orthorhombic enargite (ENG) Cu3AsS4, which has been studied in its natural mineral9 and synthetic NP10 forms. Prototype ENG-based solar cells have been fabricated from NP precursors,11 and computational work has elucidated ENG’s optoelectronic properties and accelerated the development of ideal device architectures.12–14 Another Cu-As-S phase is cubic tennantite (TEN) Cu12As4S13; it has a bandgap of 1.75 eV,7 which is too high for single-junction PV applications. However, TEN has attracted attention for its thermoelectric properties.15–17

One Cu-As-S phase that has received little attention from the research community is sinnerite (SIN), which has nominal composition Cu6As4S9. Previous experimental studies on SIN have been restricted to solving its triclinic crystal structure and measuring optoelectronic properties of amorphous Cu6As4S9 glasses.18–22 Recent theoretical studies indicate that SIN may display high absorption coefficients and thin-film PV device efficiencies exceeding 20%, as well as low lattice thermal conductivity for enhanced phonon scattering in thermoelectric applications.12,15 To the best of our knowledge, these computations have not yet been supported by measurements of the electrical and optical properties of crystalline SIN. In this work, we report the first synthesis protocol and preliminary optoelectronic characterization of SIN thin films for potential use in PV applications. SIN films were fabricated from solution-processed NP precursors and display micron-sized dense grains, an ideal bandgap (~1.2 eV) for solar energy conversion, and significant current production under simulated solar illumination. The results detailed here motivate further research and development of sinnerite thin films and PV devices, and future findings may extend to other materials in the earth abundant Cu-As-S system.

EXPERIMENTAL

Full experimental details may be found in the supplemental material (SM). Briefly, LUZ Cu3AsS4 NPs were fabricated via a hot injection method according to our group’s previous reports.7,8,11 The NPs were purified and suspended in an ink, which was blade coated onto Mo-coated soda-lime glass substrates. These substrates were then vacuum sealed in glass ampoules with commercially available As2S2 powder and heat treated at temperatures ranging from 350-500 °C. The phase purity, composition, and morphology of the thin films were studied, and the most optimal films were chosen for characterization of key optoelectronic properties.

RESULTS AND DISCUSSION

In a previous publication, we reported the first synthesis of ENG thin films with micron-sized dense grains; this was achieved by heating LUZ NPs in a sealed glass ampoule with As2S5 powder.11 At moderate temperatures (~300 – 500°C) typically used to promote grain growth in NP-based thin films, solid ENG is in equilibrium with an extensive range of liquids containing mostly As and S with a small amount (~1-3 at%) of Cu.18 The proposed mechanism for grain growth is that a liquid As-S phase initially condenses on the surface and within the nanopores of the NP film, a phenomenon driven by supersaturation of the vapor space and the nanoporosity of the initial film. This binary liquid absorbs Cu from decomposing NPs until a saturation point is reached; solid Cu3AsS4 can nucleate from this liquid either upon cooling or upon any disruption to the equilibrium. A close examination of Cu-As-S phase relations reveals that while ternary liquids are in equilibrium with Cu3AsS4 at high sulfur compositions (>55 at%), they are instead in equilibrium with Cu6As4S9 at lower sulfur compositions (~40-55 at%).18 Therefore, we hypothesized that by increasing the amount of As relative to S sealed in the ampoule, we could alter the liquid composition and form SIN, rather than ENG as seen previously.

Fig. 1 gives the grazing incidence X-ray diffraction (GIXRD) pattern of a LUZ NP film that was heated in a glass ampoule with As2S2 for 10 min at 400 °C. The major reflections suggest a tetragonal or cubic crystal structure, such as those seen in reference XRD patterns of both luzonite and lazarevicite Cu3AsS4, along with an exaggerated peak near 40° 2θ resulting from the Mo substrate. This observed pattern is not surprising – even though many additional reflections are expected due to its primitive triclinic crystal structure, SIN has a sphalerite sublattice with strong reflections that obscure signal from the true triclinic cell.19,22 Single crystals show weak peaks near 20.8°, 22.5°, 35.3°, 36.4°, 44.0°, and 45.5°; the magnified sections of the GIXRD spectra (Fig. S1, SM) suggest the presence of these peaks in these thin films, though higher resolution XRD data is needed to accurately index the minor peaks in the structure and confidently confirm a match with SIN. Additionally, none of the peaks match with elemental, binary, or ternary impurity phases that may occur in the reaction scheme used in this work.

The vastly different ideal Cu/As ratios can further distinguish between SIN (Cu/As = 1.5) and other ternary Cu-As-S phases (Cu/As = 3.0 for LUZ/ENG, ≥ 2.0 for all reported ternary phases).18 X-ray fluorescence (XRF) measurements were used to estimate the composition of as-treated thin films. For a sample treated at 400 °C for 10 min, the Cu/As ratio is 1.30, which is much closer to the stoichiometric SIN ratio than the ratio for other competing phases; however, a significant amount of excess As remains in the film. Because of the closed environment associated with the heat treatment, As-S vapors can condense on the film’s surface during cooldown, leading to artificially low Cu/As ratios. Since an aqueous solution of ammonium sulfide [(NH4)2S] dissolves arsenic sulfides,23,24 a short etch was conducted to remove any excess material from the surface. After a 1 min immersion, the Cu/As ratio increased to 1.38, indicating that As-containing phases were preferentially etched, though there still may be excess As beneath the surface of the film.

Raman spectroscopy is often used to identify the phases present in thin films, but to the best of our knowledge, a spectrum has not been reported in previous computational or experimental studies, so positive identification of SIN is not possible. However, as seen in Fig. 1(b), the Raman spectrum obtained from an As2S2-treated film etched in (NH4)2S is significantly different than that of a LUZ or ENG standard, providing further evidence that Cu3AsS4 was not formed. Additionally, the observed stretches do not align with other potential impurity phases such as copper sulfides and arsenic sulfides. It is noteworthy that an impurity peak at 494 cm-1 (corresponding to S-S bonds entrained with residual carbon) is greatly reduced in intensity when compared with our previous report on ENG films; this is likely due to reduced sulfur content in the annealing atmosphere.11 When the XRD, XRF, and Raman data are jointly considered, it is likely that Cu6As4S9 was formed from As2S2 heat treatments, rather than Cu3AsS4 or other ternary Cu-As-S phases.

For solid-state device applications, micron-sized dense grains are desirable so that the density of grain boundaries and effects of electrical shunting are minimized. Grain growth mechanisms are strongly dependent on the annealing temperatures and times. Initially, several temperatures were explored for the growth of SIN thin films over a duration of 30 minutes. Plan-view scanning electron microscopy (SEM) images (Fig. S2, SM) indicate that the 350-400 °C range is optimal for growing SIN films, as grains with relatively high packing densities are formed. Higher temperatures result in island grain growth and some decomposition to TEN (Fig. S3, SM). To further optimize the film morphology, a range of annealing times at 400 °C was tested. Fig. 2 depicts plan-view SEM images for anneals of 5, 10, 15, 30, and 60 min, all of which were identified as SIN (Fig. S4, SM). The 5 min treatment resulted in a film with significant void space, while the 60 min treatment gave a film with significant surface nonuniformity and poor grain packing. For the remainder of this manuscript, films formed from the 10 min treatment are studied, as this condition represents the best combination of uniform grain size and dense coverage. A cross-sectional SEM image (Fig. S5, SM) shows a bilayer morphology typical of many NP-based thin films, with a layer of micron-thick grains on top of a ~300 nm “fine grain” layer. This layer often contains residual carbon stemming from NP ligands,25,26 and its presence suggests that grain growth was initiated at the top of the NP film, similar to Cu(In,Ga)S2 and Cu2ZnSnS4 absorber layers that undergo liquid-assisted grain growth in a selenium atmosphere.27,28

Critical optoelectronic properties of SIN films were measured to determine the material’s relevance for semiconducting applications. To eliminate any effects resulting from carbonaceous residue, oleylamine ligands were exchanged with an As2S3-derived complex,23 and films were fabricated from these carbon-free NPs (Fig. S6, SM). One property of paramount importance for PV applications is the optical bandgap, which was estimated using diffuse reflectance spectroscopy (Fig. 3(a)). A clear decrease in the reflectance of SIN films in the near-infrared region is noted. To estimate the bandgap, the Kubelka-Munk function was used to transform the reflectance data.29 By extrapolating the function’s square to the x-axis, a direct band gap of ~1.2 eV, which is in the ideal range for solar energy conversion (1-1.5 eV), is estimated. This value is in agreement with a previous calculation of 1.19 eV,12 though future research must validate the experimental band gap through other independent measurements.

For SIN-based device applications, the energy levels of the valence and conduction bands must be measured so that an appropriate pn junction partner can be found. Cyclic voltammetry (CV) was performed on a SIN film using 0.1 M tetrabutylammonium hexafluorophosphate in acetonitrile as the electrolyte (Fig. 3(b)). The onset of current, corresponding to carrier injection to the valence band, occurs at approximately 0.4 V vs. Ag+/AgCl. The onset of ferrocene, an internal standard with an absolute redox potential of -4.80 eV vs vacuum, occurred at 0.3 V vs. Ag+/AgCl (Fig. S7, SM).30 The valence band edge of SIN, therefore, lies at approximately -4.9 eV vs. vacuum. When combined with the measured 1.2 eV band gap, the conduction band edge lies near -3.7 eV vs. vacuum. These measurements are a critical first step towards integrating SIN into prototype devices.

The photoresponse of SIN thin films was measured in a three-electrode photoelectrochemical (PEC) cell under chopped simulated AM1.5G illumination in an aqueous EuCl3 electrolyte. The stabilized current response of a SIN working electrode at a constant bias of -0.5 V vs. Ag+/AgCl is shown in Fig. 3(c). The steady generation of ~7 µA/cm2 of cathodic photocurrent indicates that SIN is a p-type material that absorbs visible and near infrared light, justifying its further development for PV applications.  The p-type nature of SIN was confirmed through hot-point probe and Hall effect measurements, the latter of which also revealed a carrier concentration of (1.7 ± 0.5) * 1019 cm-3 and a hole mobility of 0.26 ± 0.09 cm2/V*s.

Fig. 3(d) depicts the time-resolved photoluminescence (TRPL) decay of SIN films under pulsed laser illumination (λ = 637 nm). The response is well fit by a biexponential function with time constants τ1 = 334 ps and τ2 = 2.4 ns, with relative weights of 73% and 27%, respectively. This result suggests that a fraction of the minority carriers have high lifetimes, which can lead to high minority carrier diffusion lengths and greater carrier collection within a solar cell. As improvements to the SIN processing conditions are made, the carrier lifetimes are expected to improve significantly.

CONCLUSIONS

We have fabricated the first crystalline sinnerite Cu6As4S9 thin films through a heat treatment scheme that exploits equilibrium phase relations in the Cu-As-S system. The films appear to be free of detectable binary phases and possess micron-sized dense grains suitable for device applications. The films display a direct band gap around 1.2 eV, appreciable photocurrent generation under simulated sunlight, and some minority carrier lifetimes exceeding 1 ns. The valence and conduction band edges lie at -4.9 eV and -3.7 eV vs. vacuum, respectively. Future work in the development of sinnerite should focus on continued measurement of fundamental material properties, as well as finding an appropriate n-type layer to pair with SIN for a robust pn junction.

ACKNOWLEDGMENTS

The authors acknowledge the National Science Foundation for funding under grant #1534691-DMR (Rapid Design of Earth Abundant Inorganic Materials for Future PVs). S.A.M. acknowledges Purdue University for a Bilsland Dissertation Fellowship. The authors thank Kyle Weideman, Yining Feng, and Professor Luna Lu for Hall effect measurements, Joseph Andler, Essam AlRuqobah, and Xianyi Hu for providing Mo films, Apurva Pradhan for helpful comments on the manuscript, Alexei Lagoutchev for helpful discussions regarding the collection of reflectance data, and Joseph Andler for assistance with the abstract graphic. The authors declare no conflicts of interest.

SUPPLEMENTAL MATERIAL

Supplementary material is available online: safety precautions, chemical details, experimental methods, and supplemental characterization results (XRD, Raman, SEM, FTIR, and cyclic voltammetry). Additionally, the data associated with this manuscript is found at the project’s website: https://datacenterhub.org/groups/dmref1534691.

REFERENCES

1.	C. Wadia,  a. P. Alivisatos, and D. M. Kammen: Materials Availability Expands the Opportunity for Large-Scale Photovoltaics Deployment. Environ. Sci. Technol. 43(6), 2072 (2009).

2.	W. Wang, M. T. Winkler, O. Gunawan, T. Gokmen, T. K. Todorov, Y. Zhu, and D. B. Mitzi: Device Characteristics of CZTSSe Thin-Film Solar Cells with 12.6% Efficiency. Adv. Energy Mater. 4(7), 1301465 (2014).

3.	T. Gershon, T. Gokmen, O. Gunawan, R. Haight, S. Guha, and B. Shin: Understanding the relationship between Cu2ZnSn(S,Se)4 material properties and device performance. MRS Commun. 4(04), 159 (2014).

4.	C. K. Miskin, W.-C. Yang, C. J. Hages, N. J. Carter, C. S. Joglekar, E. A. Stach, and R. Agrawal: 9.0% efficient Cu2ZnSn(S,Se)4 solar cells from selenized nanoparticle inks. Prog. Photovoltaics Res. Appl. 23(5), 654 (2015).

5.	W. A. Dunlap-Shohl, Y. Zhou, N. P. Padture, and D. B. Mitzi: Synthetic Approaches for Halide Perovskite Thin Films. Chem. Rev. 119(5), 3193 (2019).

6.	T. Shi, W.-J. Yin, M. Al-Jassim, and Y. Yan: Structural, electronic, and optical properties of Cu3-V-VI4 compound semiconductors. Appl. Phys. Lett. 103(15), 152105 (2013).

7.	R. B. Balow, E. J. Sheets, M. M. Abu-Omar, and R. Agrawal: Synthesis and Characterization of Copper Arsenic Sulfide Nanocrystals from Earth Abundant Elements for Solar Energy Conversion. Chem. Mater. 27(7), 2290 (2015).

8.	R. B. Balow, C. K. Miskin, M. M. Abu-Omar, and R. Agrawal: Synthesis and Characterization of Cu3(Sb1-xAsx)S4 Semiconducting Nanocrystal Alloys with Tunable Properties for Optoelectronic Device Applications. Chem. Mater. 29(2), 573 (2017).

9.	T. Pauporté and D. Lincot: Electrical, optical and photoelectrochemical properties of natural enargite, Cu3AsS4. Adv. Mater. Opt. Electron. 5(6), 289 (1995).

10.	A. Das, A. Shamirian, and P. T. Snee: Arsenic Silylamide: An Effective Precursor for Arsenide Semiconductor Nanocrystal Synthesis. Chem. Mater. 28(11), 4058 (2016).

11.	S. A. McClary, J. Andler, C. A. Handwerker, and R. Agrawal: Solution-processed copper arsenic sulfide thin films for photovoltaic applications. J. Mater. Chem. C 5(28), 6913 (2017).

12.	L. Yu, R. S. Kokenyesi, D. A. Keszler, and A. Zunger: Inverse Design of High Absorption Thin-Film Photovoltaic Materials. Adv. Energy Mater. 3(1), 43 (2013).

13.	S. K. Wallace, K. L. Svane, W. P. Huhn, T. Zhu, D. B. Mitzi, V. Blum, and A. Walsh: Candidate photoferroic absorber materials for thin-film solar cells from naturally occurring minerals: enargite, stephanite, and bournonite. Sustain. Energy Fuels 1(6), 1339 (2017).

14.	S. K. Wallace, K. T. Butler, Y. Hinuma, and A. Walsh: Finding a junction partner for candidate solar cell absorbers enargite and bournonite from electronic band and lattice matching. J. Appl. Phys. 125(5), 055703 (2019).

15.	R. Zhang, K. Chen, B. Du, and M. J. Reece: Screening for Cu–S based thermoelectric materials using crystal structure features. J. Mater. Chem. A 5(10), 5013 (2017).

16.	S. A. McClary, R. B. Balow, and R. Agrawal: Role of annealing atmosphere on the crystal structure and composition of tetrahedrite–tennantite alloy nanoparticles. J. Mater. Chem. C 6(39), 10538 (2018).

17.	P. Levinsky, C. Candolfi, A. Dauscher, J. Tobola, J. Hejtmánek, and B. Lenoir: Thermoelectric properties of the tetrahedrite–tennantite solid solutions Cu12Sb4−xAsxS13 and Cu10Co2Sb4−yAsyS13 (0 ≤ x , y ≤ 4). Phys. Chem. Chem. Phys. 21(8), 4547 (2019).

18.	S. Maske and B. J. Skinner: Studies of the sulfosalts of copper I. Phases and phase relations in the system Cu-As-S. Econ. Geol. 66(6), 901 (1971).

19.	E. Makovicky and B. J. Skinner: Studies of the Sulfosalts of Copper II. The Crystallography and Composition of Sinnerite, Cu6As4S9. Am. Mineral. 57, 824 (1972).

20.	J. Hautala and P. C. Taylor: A review of optical properties of metal chalcogenide glasses. J. Non. Cryst. Solids 141(C), 24 (1992).

21.	B. Yan, S. Girlani, and P. C. Taylor: Defect structure and conductivity in tetrahedrally coordinated metal chalcogenide amorphous semiconductors. Phys. Rev. B 56(16), 10249 (1997).

22.	L. Bindi, E. Makovicky, F. Nestola, and L. De Battisti: Sinnerite, Cu6As4S9, from the Lengenbach Quarry, Binn Valley, Switzerland: Description and Re-Investigation of the Crystal Structure. Can. Mineral. 51(6), 851 (2013).

23.	M. V. Kovalenko, M. I. Bodnarchuk, J. Zaumseil, J.-S. Lee, and D. V. Talapin: Expanding the Chemical Versatility of Colloidal Nanocrystals Capped with Molecular Metal Chalcogenide Ligands. J. Am. Chem. Soc. 132(29), 10085 (2010).

24.	Z. Xia, J. Zhong, M. Leng, L. Hu, D.-J. J. Xue, B. Yang, Y. Zhou, X. Liu, S. Qin, Y.-B. B. Cheng, and J. Tang: Generalized Water-Processed Metal Chalcogenide Complexes: Synthesis and Applications. Chem. Mater. 27(23), 8048 (2015).

25.	W. Wu, Y. Cao, J. V Caspar, Q. Guo, L. K. Johnson, I. Malajovich, H. D. Rosenfeld, and K. R. Choudhury: Studies of the fine-grain sub-layer in the printed CZTSSe photovoltaic devices. J. Mater. Chem. C 2(19), 3777 (2014).

26.	T. J. Huang, X. Yin, C. Tang, G. Qi, and H. Gong: Influence of Ligands on the Formation of Kesterite Thin Films for Solar Cells: A Comparative Study. ChemSusChem 9(9), 1032 (2016).

27.	C. J. Hages, M. J. Koeper, C. K. Miskin, K. W. Brew, and R. Agrawal: Controlled Grain Growth for High Performance Nanoparticle-Based Kesterite Solar Cells. Chem. Mater. 28(21), 7703 (2016).

28.	S. McLeod, E. Alruqobah, and R. Agrawal: Liquid assisted grain growth in solution processed Cu(In,Ga)(S,Se)2. Sol. Energy Mater. Sol. Cells 195(February), 12 (2019).

29.	P. Kubelka and F. Munk: Ein Beitrag zur Optik der Farbanstriche (Contribution to the optic of paint). Zeitschrift fur Tech. Phys. 12, 593 (1931).

30.	R. R. Gagne, C. A. Koval, and G. C. Lisensky: Ferrocene as an Internal Standard for Electrochemical Measurements. Inorg. Chem. 19(9), 2854 (1980).

CAPTIONS

FIG. 1. (a) GIXRD and (b) Raman spectrum of a luzonite Cu3AsS4 NP film that was treated in an As2S2 atmosphere at 400 °C for 10 min. The GIXRD pattern agrees with a reference standard for sinnerite Cu6As4S9 (ICSD collection code 236895) and is free of detectable impurity phases. The peak marked with (*) is exaggerated in intensity due to the Mo substrate. The Raman spectrum is significantly different than that of those reported for Cu3AsS4 minerals (RRUFF ID R060390 and R050373).

FIG. 2. Plan-view SEM images of LUZ NP films heated with As2S2 at 400 °C for 5, 10, 15, 30, and 60 min.

FIG. 3. Optoelectronic characterization of sinnerite Cu6As4S9 thin films. (a) Diffuse reflectance spectroscopy data and Tauc plot of the Kubelka-Munk function. Linear extrapolation gives a direct band gap of ~1.2 eV. (b) Cyclic voltammetry in 0.1 M tetrabutylammonium hexafluorophosphate in acetonitrile electrolyte solution. The current onset occurs at ~0.4 V vs Ag+/AgCl. (c) Photoelectrochemical current generation in aqueous EuCl3 electrolyte under chopped AM1.5G illumination. (d) Time-resolved photoluminescence decay and biexponential fit to the measured data.